MICA TAPE SERIES

| Phlogophite, TYPE- CP25G Temp rating: 750 °C to 800 °C Std used - IEC 60331-1/2/3/21 |  | Phlogophite + Inorganic, TYPE- CP25GE Temp rating: 750 °C to 950 °C Std used -BS 6387 CWZ, IEC 60331- 1/2/3/21, BS EN 50200 |  |
| --- | --- | --- | --- |
| Muscovite, TYPE-CM25G Temp rating: 950 °C Std used -BS 6387 CWZ |  | Muscovite + Inorganic, TYPE-CCM25GE Temp rating: 950 °C to 1200°C Std used -BS 7846, BS EN 50200, BS 8434-2 |  |
| Glass + Muscovite + Glass, TYPE-CM25DG Temp rating: 950°C Std used -BS 6387 CWZ |  | Muscovite Calcined TYPE-CCM25G Temp rating: 950°C Std used -BS 6387 CWZ, BS EN 50200 |  |

Mica Taping on Conductor

Chhaperia tapping Facility, The Fully automatic Mica Tapping facility in the industry at Chhaperia . Our mica-taped conductors utilize premium mica tape to deliver exceptional insulation properties, particularly in high-temperature environments. Experience enhanced conductor reliability with our mica taping services. Our mica taping process creates a robust insulation barrier around conductors.

Chhaperia Tapping Feature

- Conductor Supplied by the Customer.

- Tapping service as per customer specification.

- Inhouse Facility of Fire Testing Lab.

Chhaperia Mica Tape which can meet various Standard as below: -

Type              Suitable for

CP25G         IEC 60331-1/2/3/21

CM25G        BS 6387 (C W & Z)

CP25GE       BS 6387 (C W & Z), BS EN 50200,

CCM25GE      BS 6387 (C W & Z), BS 7846 (CATEGORY F2, F120) & BS 8434-2

(CAT- ph120 & Annex E)

Tapping Ranges of Conductor: - 0.5 SQMM to 20 SQMM.

Overlapping %: - 10 to 50% Coverage %: - 100  No of Layer: - 1 to 3

Water Blocking Tape Series

Non-Conductive

| Type- CHSNW 15 T- 0.2mm T.S – 25 to 30N/cm GSM- 55 E- 11% S/S- 5 S/H- 8 |  | Type- CHDNW 20 T- 0.2mm T.S – 25 to 30N/cm GSM – 80 E – 11 % S/S – 10 S/H – 15 |  |
| --- | --- | --- | --- |
| Type- CHDNW 25 T – 0.25mm T.S- 35N/cm GSM- 90 E- 11% S/S- 10 S/H- 14 |  | Type- CHDNW 30 T- 0.30mm T.S – 35 N/cm GSM – 100 E – 11 % S/S – 10 S/H – 12 |  |
| Type- CHDNW-R1225 T – 0.25mm T.S- 80 N/cm GSM- 100 E- 17% S/S- 10 S/H- 14 |  | Type- CHDNW-30R T- 0.28mm T.S – 100 N/cm GSM – 100 E – 15 % S/S – 10 S/H – 15 |  |
| Type- CHDNW-28CAB T – 0.28mm T.S- 30 N/cm GSM- 60 E- 13% S/S- 8 S/H- 9 |  |  |  |

Water Blocking Tape Series

Semi-Conductive

| Type- CHDSW 25 T – 0.25mm T.S- 35N/cm GSM- 100 E- 12% S/S- 10 S/H- 15 S/R ≤ 1500 Ω |  | Type- CHDSW 30 T- 0.3mm T.S – 40N/cm GSM – 110 E – 12 % S/S – 8 S/H – 12 S/R - ≤1500 Ω |  |
| --- | --- | --- | --- |
| Type- CHDSW 35 T – 0.35mm T.S- 40N/cm GSM- 135 E- 12% S/S- 12 S/H- 15 S/R - ≤1500 Ω |  | Type- CHDSW 4189CAB T- 0.40mm T.S – 45 N/cm GSM – 100 E – 12 % S/S – 6 S/H – 8 S/R - ≤1500 Ω |  |
| Type- CHDSW41CAB T – 0.40mm T.S- 50 N/cm GSM- 110 E- 12% S/S- 8 S/H- 10 S/R - ≤1500Ω |  | Type-CHDSW40R T- 0.40mm T.S – 80 N/cm GSM – 160 E – 14 % S/S – 12 S/H – 16 S/R - ≤1500 Ω |  |

Semi-Conductive Woven Tape

| Type- CHSCWWBT 15 T – 0.15mm T.S- 120N/cm GSM- 130 E- 20% S/S- 4 S/H- 6 S/R - ≤2000 Ω |  | Type- CHSCWWBT 22 T- 0.22mm T.S – 180N/cm GSM – 180 E – 20 % S/S – 5 S/H – 3 S/R - ≤2000 Ω |  |
| --- | --- | --- | --- |

Copper wire woven Semi-Conductive WBT Tape

| Type- CHCWSCWBT 35 T – 0.35mm T.S- 500 N/Width GSM- E- 5 % S/S- 3 S/H- 5 S/R - ≤1500 Ω |  | Type- CHCWSCWBT 45 T- 0.45mm T.S – 500N/Width GSM - E – 20 % S/S – 5 S/H – 3 S/R - ≤2000 Ω |  |
| --- | --- | --- | --- |

Semi Conductive Non-Woven Tape

| Type- CHCNW-12 T – 0.12mm T.S- ≥18 N/cm GSM- 45 E- 10 % S/R - ≤2000 Ω |  | Type- CHCNW-20 T- 0.2mm T.S – ≥35N/cm GSM - 60 E – 12 % S/R - ≤2000 Ω |  |
| --- | --- | --- | --- |

Semi Conductive Woven Tape

| Type- CHN 20 R T – 0.20mm T.S- ≥200 N/cm GSM- 170 E- 25 % S/R - ≤1000 Ω |  | Type- CHN 12 R T- 0.12mm T.S – ≥120 GSM - 100 E – 20 % S/R - ≤1500 Ω |  |
| --- | --- | --- | --- |
| Type- CHN 20 HT T – 0.20mm T.S- ≥300 N/cm GSM- 170 E- 25 % S/R - ≤1500 Ω |  | Type- CHN 12 S T- 0.12mm T.S – ≥120 GSM - 100 E – 20 % S/R - ≤2000 Ω |  |

Semi Conductive Water Blocking Foam Tape

| Type- CHSMWBT-F-100 T – 1.0mm T.S- ≥35 N/cm GSM- 270 E- 12 % S/R - ≤1500 Ω |  | Type- CHCNW-125 T- 1.25mm T.S – ≥40N/cm GSM - 300 E – 12 % S/R - ≤1500 Ω |  |
| --- | --- | --- | --- |
| Type- CHSMWBT-F-150 T – 1.5mm T.S- ≥40 N/cm GSM- 350 E- 12 % S/R - ≤1500 Ω |  |  |  |

Other Tapes

| NAME-LSZH, Low Smoke Zero Halogen FIBER GLASS TAPE Type- CHPBT Thickness: 0.10 |  | NAME- Polyester Binder Tape Type- CHLSZH Thickness Range – 0.10 to 0.12 mm |  |
| --- | --- | --- | --- |
| NAME- POLY FIBER GLASS TAPE Type- CHPFG Thickness Range – 0.14 to 0.16 mm |  | NAME- FIBER GLASS TAPE Type- CHFGT Thickness Range- 0.10 to 0.60mm |  |
| NAME- COTTON TAPE Type- CHCT Thickness – 0.14 mm |  | NAME- BITTUMINIZED TAPE Type- CHBCT Thickness Range- 0.20 to 0.40mm |  |
| NAME- ALUMINIUM MYLAR TAPE Type- CHALPET Thickness Range – 0.025 to 0.10mm |  | NAME- POLYESTER TAPE Type- CHPET Thickness Range- 0.15 to 0.2mm |  |
| NAME- NON-WOVEN FLEECE TAPE Type- CHNW Thickness Range – 0.05 to 0.20mm |  | NAME- FOAMED PP TAPE Type- CHFPP Thickness Range- 0.08 to 0.2mm |  |